FLOWCHART OF MANUFACTURING PROCESS & SCHEME OF TESTING
(XLPE- CABLE)
RAW MATERIAL
XLPE





 SPECFIC-GRAVITY, HOT SET


T.S & ELONGATION





ALU/COPPER





G.I.WIRE/STRIP





G.I.WIRE/STRIP





FINISH, DIMENSION UNIFORMITY OF ZINC COATING, T.S & ELONGATION











PVC





SPECIFIC GRAVITY THERMAL STABILITY


LOSS OF MASS T.S & ELONGATION (BEFORE & AFTER AGEING)





FINISH, SIZE, COND RESISTANCE, WRAPPING & TENSILE (FOR ALUM) ANNEALING (FOR COPPER)





STRANDING





STRANDING





DIMENSIONS, CONDUCTOR RESISTANCE & WEIGHT





CORE INSULATION





(CURING (XLPE)





 FINISH, DIMENSIONS, THICKNESS, SPARK TESTING 





LAYING UP





SEQUENCE & DIRECTION OF LAY CIRCULARITY & DIA OVER LAID UP CORES





INNER SHEATHING





FINISH, CONCENTRICITY, THICKNESS, DIA OVER INNER SHEATH





ARMOURING





FINISH, NO. OF WIRES/STRIPS, DIRECTION OF LAY, DIA OVER ARMOUR, HIGH VOLTAGE





FINAL SHEATHING





FINISH, EMBOSSING, CONCENTRICITY, THICKNESS, OVERALL, DIAMETER





TESTING





ROUTINE TESTING





ON ALL CABLE LENGTHS





 TYPE TESTING





ON SAMPLE FORM EACH SIZE & TYPE OF CABLE





 TESTED OK CABLE





ON SAMPLE FORM EACH SIZE & TYPE OF CABLE





 FINAL PACKING & SEALING





RAW MATERIAL








