XLPE Vs PVC – COMPARATIVE PROPERTIES SUMMARY

| Properties | XLPE | PVC |
| --- | --- | --- |
| 1. Chemical Structure 2. Polymer Structure 3. Temperature Rating Degree C a) Operating b) Emergency overload c) Short Circuit 4. Cable Installation Job 5. Current Carrying Capacity 6. Dielectric Strength (KV/mm) 7. Volume Resistivity (ohm-cm) 8. Thermal Resistivity (Deg C/cm/watt) 9. Dielectric Constant at 20 Deg. C2.3 10.Power Factor at 20DegC X1013 11. Low Temperature Brittleness Deg. C 12. Moisture Penetration Resistance 13. Oil Resistance 14. Solvent Resistance 15. Acid Resistance 16. Alkali Resistance | Themoset, pure Hydrocarbon. Non-Polar C-C or Si-o-Bonds Partial Crystalline 90 130 250 Easy due to less Wt, less Diam and Less Bending radius. 30% Higher than PVC 550 1017 350 7.4 0.4 -90 Excellent Excellent Excellent Excellent Excellent | Thermoplastic Polar Rotosenated. C.Ci. Bond Amorphous 70 90 135 350 1014 730 80 -15 Good Fair Poor Fair Good |